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DESCRIPTION: 
ECO RAPID is an innovative and eco-friendly self-levelling industrial floor. 
Hardens fast and tension-relieved with a layer thickness of 2 – 50 mm. 
COLOR:  
The original color of ECO RAPID is grey.  
	PROPERTIES AND BENEFITS 
• High mechanical load 
• Good chemical & saltwater resistance 
• Fast curing, crack & shrinkage free 
• Made with alternative materials that have a low CO2 footprint.  
• Non-hazardous material with no allergy potential 
• Fulfills the requirements for discharge capability according to DIN EN 61340-5-1  • Waterproof up to 1.5 bar. 
• Very low emission EMICODE EC 1PLUS 
• Odorless 
• Walkable after 4 hours & fully loadable after 4 days 
• Very high adhesion, compressive & tensile strength 
• Also process able by machine




RANGE OF USAGE 
ECO RAPID is ideal for all concrete and cement based indoor areas. Outdoor use is also possible. It is suitable  for locations with high mechanical, chemical loads and high abrasion such as industrial floorings, warehouses,  production areas, garages and hospitals. Smooth layers between 2 – 50 mm, a layer thickness of approx. 3 – 5  mm is recommended.
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TECHNICAL INFORMATION 
Strength class CT-C50-F10 according to  
DIN EN 13813 Mixing ratio 4.5 L water per 25  
kg powder 
Abrasion resistance  
according to Böhme A9  
Strength 
Compressive strength Flexural strength 
approx. 50 N/mm² approx. 10 N/mm2  
Processing time at 20°C Processing temperature 
approx. 35 min 
Min. +2 °C, max. +35 °C 
Slip resistance Without quartz sand With quartz sand 
R 10 
R 13 / V8 
approx. 1.8 kg / m²  
Application thickness 2 - 50 mm Consumption  
and mm layer  thickness 
Loadability 
Walkable  
Light load 
Fully loadable 
Fully loadable in exterior  areas 
Curing at 20°C after 4 hours 
1 day 
4 days 
7 days 
Density 
Bulk density 
Fresh mortar density 
approx. 1.2 kg/dm3  approx. 2.0 kg/dm3 
The information above is given based on our experiences. Adjustment may be required in case of object specific  fluctuations. 
PREPARATION OF SUBSTRATE 
Prior to coating process, ensure that the surface is dry and clean and free from all kinds of separating agents.  Mechanical surface preparation for example shot-blasting is recommended. Deeper ruptures must be filled with  ECO REPAIR. The surface should be permanently vibration-free and crack-free. Already existing cracks must be  repaired professionally. The pull of test should be min. 1.5 N/mm2. For priming the concrete surface must be dry.  The substrate must be dried for 2 hours after priming with ECO PRIMER. By priming the surface, the  absorbency of the substrate is adjusted. This avoids the rising of air bubbles during the subsequent coating. In  order to guarantee this on critical undergrounds, a test area of 1 m2 should be created. Apply a further layer of  primer if necessary. The coating work on primer must be finished within 6 hours.  
For simultaneous work on different substrate apply first a 1 mm layer this is to avoid too much different coloring  and absorbencies and wait 6 hours before priming again. 
Before the second layer please prime again to avoid bubbles, expansion joints are to take over. Prepare ceilings,  walls, windows and doors suitable for the decorative fresh mortar surface and protect it from dust and insects. 
MIXING AND APPLICATION 
First, add 4.5 liters of water per 25 kg powder material into the mixing container. Then, pour powder inside while  stirring. For manual applications use a suitable handheld mixer. We recommend using the mixing paddle  COLLOMIX DLX 152 HF. By using the respective mixing paddle, a proper thread adapter must be used. The  material has to be mixed intensely for 2 minutes, left to set for 2 minutes, and then mixed again for 1 more  minute. Single mixing batches must be mixed fast and uniform. The material has to be poured out seamlessly. 
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within the workability time. With manual processing an aeration time of up to 5 minutes has to be maintained  between the end of the mixing time and application of the material. This minimizes rising of air bubbles within  the poured material. The use of a continuous mixing pump or a semi-automatic charge mixer is required for  large areas. Mixing time for the semi-automatic charge mixer is approximately 4 to 6 minutes per 100 kg  powder. 
After mixing, apply ECO RAPID onto the primed surface and distribute it with a pin leveler to the intended  thickness. In order to avoid processing marks in the fresh surface use a surface scraper to smoothen the  surface. Use a thin spiked roller on the freshly laid mortar for better levelling and deaeration. Consider the  spikes to be long enough. 
For optimal leveling of the fresh mortar and to maintain the flatness tolerances according to NBN ISO 7976-1 it  is recommended to use a layer thickness of approximately 3 – 5 mm for larger areas. Thereby the required layer  thickness depends on the surface quality of the substrate which has to be coated. The coating has to be  protected from too quick drying (solar radiation, draft), frost and rain for the 1st 24 hours. Do not cover the  finished surface with foils or other materials. 
Use disposable overshoes to protect the surface until sealed against dirt and moisture. 
Note concerning post-processing and coating protection: To achieve a higher abrasion resistance or  chemical resistance we recommend a combined application of ECO HYDRO SIL and ECO HYDRO GLASS or  ECO TOPCOAT MAT. Please refer to the respective data sheets for more information.  
TOOLS AND CLEANING 
Mixing device (drill mixer or pump), trowel, spiked shoes, spiked roller and screed rake or pin leveler. All equipment should be washed clean and dried before and after application. 
PACKAGING AND STORAGE 
Packaging: 25 kg bag 
Storage: 12 months in original packaging and in a dry, moisture-free environment. 
SAFETY, ECOLOGY AND ELIMINATION 
There is no mandatory hazard labeling for ECO RAPID. Avoid inhaling dust when opening packaging. Protect  skin and eyes during the mixing process. Please refer to the Material Safety Data Sheet (MSDS) which can be  requested on www.ets-europe.be for further information on safety during transportation, storage, handling and  disposal. Follow instructions on the packaging. 
NOTES 
Some minor color differences are inevitable due to different production batches. This should be taken into  account while performing work. It is necessary to work on designated sections with the same batch (see label) if  a uniform color is desired. Due to different water addition during application or changing working techniques light 
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color shades in the coating surface can occur. Please take note that this coating is a mineral/inorganic product.  Avoid inhaling dust when opening packaging. Protect skin and eyes during the mixing process. Please refer to  the Material Safety Data Sheet (MSDS) for further information on safety during transportation, storage, handling  and disposal. Follow instructions on the packaging. 
The content of this technical data sheet corresponds to the latest development and our applications experience. All information is based on  ideal conditions and therefore does not apply for every application purpose. Due to different materials, substrates and different actual site  conditions no warranty is given for the customer’s application. In particular, we assume no liability based on this information or any verbal  statements. The only exception is when we can be blamed for the case of intent or gross negligence. In that case the customer has to prove  that he has transmitted all required information completely and in a timely manner for a proper and promising evaluation by ETS Europe. Any  further details regarding the application of our products have to be confirmed in writing by ETS Europe. The customer must test the product’s  suitability for the intended application and purpose. We reserve the right to change the product specifications due to the ongoing  development. Apart from that our general terms and conditions are valid. This data sheet supersedes all earlier technical data on this  product. The technical data sheet can be requested on www.ets-europe.be.
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No. ECO RAPID

	EN 13813 
EN 13813 CT-C50-F10-A9 
Innovative and eco-friendly self-levelling  industrial floor. Hardens fast and tension relieved with a layer thickness of 2 - 50  mm.

	Fire behavior 
	A1

	Compressive strength 
	C50

	Flexural strength 
	F10

	Release of corrosive 
substances 
	CT
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